# Deepdek 40 Aluminum Corrugated Sheet

Deepdek 40 Profile

The roofing panel shall have a cover width of 915mm. Nominal rib height shall be 40mm. The ribs shall have a nominal pitch of 183 mm center to center and with anti-capillary side lap feature.

#### Aluminum Grade

The aluminum cladding shall be roll-formed 1.0mm thick (Bare Metal Thickness) and comply with BS EN 485 3003-H24 with follow mechanical properties.

Ultimate Stress P= 145MPa

0.2% Proof Stress, Po=115MPa

Shear Stress, Pv=69MPa

PVDF Coating

Coating Class is High performance Polyvinylidene Fluoride (abbreviated PVDF or called Fluorocarbon)

Top coat – Advance durability polyester paint of >µ25m

Reverse coat – Shadow Grey wash coat of >6µm

Costing Bending test: No crack for 90 degree bending

Pencil Hardness Test =2H

Warranty

Material warranty issued from manufacturer for material will have a life prior to perforation by weathering in the natural elements of 20 years. No cracking, flaking or peeling of the paint under warranty period provided the roofing/walling sheets are normally well-washed exposure conditions.

# Flashing

# All flashing shall be manufactured by Roofing Supplier.

# Flashing, capping and trims shall be manufactured from same type or similar standard of finished materials as the profiled steel sheet.

# Galvanized notched subgirt

The purlin support for the roofing sheet to be Zed Sections are cold-roll steel complying with AS1397-1993.

Steel grade to be G450 (450MPa yield strength), min. Z275 zinc coating (275g/m2 min. coating mass)

# Thermal & Acoustic Insulation

# The thermal & acoustic insulation layer to be 50mm thick, 24kg/m3 density fibreglass.

# Sealant

Sealants shall be an approved adhesive material, suitable for application on all aspects, of a consistency suitable for application by means of trowel, knife or gun available as a preformed strip or tape for providing a seal between a unit or structure.

The sealant should have the following properties:

- Elasticity to accommodate expected movement of the substrate materials;

- Adhesion to joint surfaces:

- Waterproof;

- Durable to UV light;

- Able to act as an anti-corrosion barrier between dissimilar material;

- When cured, stays rubber from 60 to 200 oC without tearing, cracking, drying out or become brittle;

- Sealant to conform to ASTM C-920 & BS 5889

# Fasteners

Fastener for the roofing sheets & flashing shall be proprietary SS 316 M5 Stainless Steel self-drilling with bond washer and tapping screw recommended by the Roofing Manufacturer.

# Quality Assurance

- The roofing installer shall be currently approved by the manufacturer of the roofing material.

- For actual installation of roofing, use only competent and skilled roofer completely familiar with and experienced in the application of the materials specified herein.

- The manufacturer shall be an ISO 9002 accredited company.

- The roofing works shall be carried out by a specialist firm having a minimum 5 years local experience in double standing seam roofing project.